ALL SLIDING DOORS

PART 1 GENERAL

1.1    SECTION INCLUDES

A.	Single frameless glass sliding doors (UNIKGLASS / POCKETGLASS / KTGLASS EXPERT / UNIKSELF)

B.	Frameless glass sliding doors with fixed glass sidelights (ROLLGLASS)

C.		Bi-Parting frameless glass sliding doors (UNIKMATIC / ROLMATIC)

- Telescopic frameless glass sliding Doors (EXTENDO)

- All wood, metal and framed glass sliding doors (SLID)

1.2   REFERENCES

- ANSI Z97.1 Safety Glazing Materials Used in Buildings - Safety Performance Specifications and Methods of Tests

- ASTM C 1036 Specification for Flat Glass

- ASTM C 1048 Specification for Heat-Treated Flat Glass - Kind FT

- CPSC 16 CFR 1201 Architectural Glazing Standards and Related Materials.

- Section 05120 : Structural Steel : Track supports

- Section 08120 : Aluminum Doors and Frames : Aluminum doors for sliding applications

- Section 08211 : Flush Wood doors : Wood doors and panels for sliding and folding door and walls

1.3    DESIGN / PERFORMANCE REQUIREMENTS

A.	Deflection: Limit deflection to flexure limit of glass with full recovery of glazing

1.4    SUBMITTALS

A.            Submit under provisions of Section 01300

B.            Product Data: Manufacturer's data sheets on each product to be used, including:

1.       Preparation instructions and recommendations.

2.       Storage and handling requirements and recommendations

3.       Installation methods.

C.            Shop Drawings:

- Include plans, elevations, sections, and details.

- Indicate dimensions, weights, and required installation.

- Indicate details of track and door connections, rail sections, fittings and hardware  components.

4.        Indicate glass type, sizes and details.

5.        Indicate location and installation requirements for hardware and track including                  floor tolerances required and direction of travel.

D.	 	 Verification Samples: For each finish product specified, two samples, representing actual        product finishes.

- Aluminum extrusions: on request 7” (200 mm) long sections of rails and other items.

E.	 	Manufacturer's Certificates: Certify products meet or exceed specified requirements.

F.		Manufacturer’s warranties.

G.		Contract Closeout: Submit

- Manufacturer's Warranty.

- Parts lists and installation instructions including data on operating hardware.

1.5    QUALITY ASSURANCE

- Manufacturer Qualifications: Glass door manufacturer to have minimum five years documented experience in the fabrication of glass doors of the type required for this project and be capable of providing field service representation during installation.

- Installer Qualifications: Experienced installer to have minimum five years documented experience in the work of this section and who has specialized in the installation of work similar to that required for this project.

1.6    DELIVERY, STORAGE, AND HANDLING

- Store products in manufacturer's unopened packaging until ready for installation in dry, protected and well ventilated area.

- Protect materials from damage and exposure to moisture.

1.7    PROJECT CONDITIONS

- Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's absolute limits.

- Field Measurements: Verify opening dimensions of all-glass entrances by field measurements before fabrication and indicate the measurements on Shop Drawings. Coordinate fabrication schedule with construction progress to avoid delaying the work.

1.8    WARRANTY

A.	Provide written warranty signed by the fabricator of the glass doors and glass door systems agreeing to provide a two year warranty covering replacements of those doors that develop manufacturing defects defined as any defect materially obstructing vision through the glass, and any mechanical failure of hardware which prevents the proper operation of the doors and appropriate installation.

1.9    COORDINATION

- Coordinate work with other operations and installation of adjacent surfaces to avoid damage to installed materials.

- Coordinate work with adjacent floor, wall, and ceiling construction to accommodate frame anchorage, panel track, and concealed hardware.

- Coordinate work with concrete floors and floor finishes for adequate tolerances and clearances between door panels and floor finish.

PART 2 PRODUCTS

2.1    MANUFACTURERS

A. Acceptable Manufacturer: KLEIN USA Inc., which is located at: 833 Magnolia Ave; Elizabeth, NJ 07201; Toll Free Tel: 888- KLEN US; Tel: 908 994 1111; Email: info@klein-usa.com; Web: www.klein-usa.com

B.	Substitutions: Not permitted

2.2    GLASS PRODUCTS

A.	General:

- Safety Glazing Standard: Provide fully tempered glass, Kind FT, compiling with ASTM C 1036 and ASTM C 1048 requirements, including glass indicated by reference to type, class, quality.

- Sizes: Fabricate glass to size required for openings indicated, with edge clearances and tolerances complying with recommendations of glass and hardware manufacturer.

- Provide glass types and thickness as indicated on the drawings.

2.3    ALL FRAMELESS GLASS, WOOD AND FRAMED GLASS SLIDING DOORS

- Single frameless glass sliding doors (UNIKGLASS / POCKETGLASS / KTGLASS EXPERT / UNIKSELF)

1.	System for single top hung frameless glass door including track and complete set of accessories in a single kit.

2.	Track: Clear anodized aluminum finish with track's length of 78, 118" or 157". Custom finish and size on request for project over 100 doors (custom fabrication)

- Unikglass 60 for 60kgs panel (132 lbs). Size 2" (51 mm) high x 1 5/16" (34mm) wide

- Unikglass 90 for 90kgs panel (200 lbs). Size 2 7/8" (73mm) high x 1 9/16" (40mm) wide

- Unikglass 100 for 100kgs panel (220lbs). Size 2 7/16" (62mm) high x 2" (51mm) wide

- Pocket Glass for 130kgs panel (286lbs). Size tracks 1 3/4" (45mm) x 1 3/8" (36mm) wide

- KT Glass Expert for 180kgs (400 lbs). Size tracks 7 3/8" (188mm) x 1 11/16" (43mm) wide

- Unikself. Size tracks 3 3/8" (85mm) high x 3 3/16" (80mm) wide

3.	Carriers: Top hung clamp-on roller carriers (with Full Ball Bearings wheels), two per panel, pressure applied (no glass drilling)

4.	Hardware including in the kit:

- 2 pressure clamps with rollers for one sliding door

- Stoppers-brakes

- 1 floor guide (2" wide)

- Upper track with clipped valance and end caps (except for Pocket Glass)

5.	Door Panels: Maximum weight capacity indicated on each product to reach an opening and closing force of maximum 5 lbs (23n) to fit ADA requirements.

6.	Door Panel Glazing:

a.	Clear Glass: Conforming to the requirements.

- ASTM C1048, Kind FT (fully tempered), Condition A (uncoated surfaces), Type 1 (transparent), Class 1 (clear) requirements.

- Provide products that have been tested for surface and edge compression according to ASTM C 1048 and for impact strength according to CPSC 16 CFR, part 1201 for Category II materials.

b.	Door cutouts: No drillings necessary

c.	Thickness:

- 3/8 inch (10mm)

- ½” inch (12.7mm)

- Exposed Edges: Flat polished.

- Frameless glass sliding doors with fixed glass sidelights (ROLLGLASS)

- System for top hung frameless glass door(s) sliding along fixed glass panels including track and complete set(s) of accessories in a single kit. A single track includes fixed and sliding glass panel for an easier, faster and nicer installation.

- Track: Clear anodized aluminum finish with track's length of 118" or 157". Custom finish on request for project over 100 doors (custom fabrication)

a.	Rollglass 40 for 40kgs panel (88 lbs). Size 2 3/8" (60mm) high x 1 5/8" (41 mm) wide

b.	Rollglass 90 for 90kgs panel (200lbs). Size 3 1/8" (80mm) high x 1 7/8" (47mm) wide

c.	Rollglass 100 for 100kgs panel (220lbs). Size 2 13/16” (72mm) x 2 5/16” (58.5mm) wide

d.	Rollglass 135 for 135kgs panel (300lbs). Size 3 3/4" (95mm) high x 2 1/16" (52mm) wide

e.	Rollglass 175 for 175kgs panel (375lbs). Size 3 3/4" (95mm) high x 2 1/16” (52mm) wide

3.	Carriers: Top hung clamp-on roller carriers (with Full Ball Bearings wheels), two per panel, pressure applied (no glass drilling)

4.	Hardware including in the kit:

- 2 pressure clamps with rollers 1 sliding door

- Stoppers-brakes

- 1 guide (2" wide)

- Bottom extrusion to handle fixed glass panels

- Upper track with clipped valance (valance replaced by a security seal for recessed application)

5.	Door Panels: Maximum weight capacity indicated on each product to reach an opening and closing force of maximum 5 lbs (23n) to fit ADA requirements.

6.	Door Panel Glazing:

a.	Clear Glass: Conforming to the requirements.

- ASTM C1048, Kind FT (fully tempered), Condition A (uncoated surfaces), Type 1 (transparent), Class 1 (clear) requirements.

- Provide products that have been tested for surface and edge compression according to ASTM C 1048 and for impact strength according to CPSC 16 CFR, part 1201 for Category II materials.

b.	Door cutouts: No drillings necessary

C.	Thickness:

- 3/8 inch (10mm).

- 1/2" inch (12.7mm)

d.	Exposed Edges: Flat polished.

- Bi-Parting frameless glass sliding doors (UNIKMATIC / ROLMATIC)

1.	System for bi-parting top hung frameless glass doors sliding simultaneously along a wall (Unikmatic) or along glass sidelights (Rolmatic) including track and complete set(s) of accessories in a single kit. Synchronized gear already included and pre-mounted into the track for a faster, easier and nicer installation.

2.	Track: Clear anodized aluminum finish with track's length of 118", 157" or 196". Custom finish on request for project over 100 doors (custom fabrication)

- Unikmatic for 90kgs panel (200 lbs). Size 3 3/8" (85mm) high x 2 1/8” (54mm) wide

- Unikmatic Comer for 90kgs panel (200 lbs). Size 3 3/8" (85mm) high x 2 1/8" (54mm) wide for 90° corner application

- Rolmatic for 90kgs panel (200 lbs). Size 4 1/8" (105mm) high x 2 7/16" (65mm) wide

- Rolmatic Comer for 90kgs panel (200 lbs). Size 4 1/8" (105mm) high x 2 7/16" (65mm) wide for 90° corner application

3.	Carriers: Top hung clamp-on roller carriers (with FA Ball Bearings wheels), two per panel, pressure applied (no glass drilling)

4.	Hardware including in the kit:

- 4 pressure clamps with rollers

- Stoppers-brakes

- 2 guides (2” wide)

- Bottom extrusion to handle fixed glass panels for Rolmatic only

- Upper track with clipped valance and pre-installed gear

5.	Door Panels: Maximum weight of 200 lbs/door to reach an opening and closing force of maximum 5 lbs (23n) to fit ADA requirements.

6.	Door Panel Glazing:

a.	Clear Glass: Conforming to the requirements.

- ASTM C1048, Kind FT (fully tempered), Condition A (uncoated surfaces), Type 1 (transparent), Class 1 (clear) requirements.

- Provide products that have been tested for surface and edge compression according to ASTM C 1048 and for impact strength according to CPSC 16 CFR, part 1201 for Category II materials.

b.	Door cutouts: No drillings necessary

C.	Thickness:

- 3/8 inch (10 mm)

- 1/2 inch (12.7mm)

d.	Exposed Edges: Flat polished.

- Telescopic frameless glass sliding Doors (EXTENDO)

1.	System for telescopic top hung frameless glass doors sliding simultaneously, 2, 3 or 4 panels along a wall, a glass sidelights or a pocket wall including track and complete set(s) of accessories in a single kit. Synchronized gear already included and pre-mounted into the track for a faster, easier and nicer installation.

2.	Track: Clear anodized aluminium finish with track's length of 98, 118", 137, 157" or 196". Custom finish on request for project over 100 doors, (custom fabrication)

a.	Track' size from 4 11/16" (119mm) high x 3 3/8" (86mm) wide

3.	Carriers: Top hung clamp-on roller Carriers (with Full Ball Bearings wheels), two per panel, pressure applied (no glass drilling)

4.	Hardware including in the kit:

- 2 pressure clamps with rollers / sliding door

- Stoppers-brakes

- 1 guide / sliding door (2" wide)

- Bottom extrusion to handle fixed glass sidelights

- Upper track with pre-installed gear

5.	Door Panels: for glass panels up to 3m (10') high. Total opening from 50" to 100" to reach an opening and closing force of maximum 5 lbs (23n) to fit ADA requirements.

6.	Door Panel Glazing:

a.	Clear Glass: Conforming to the requirements.

- ASTM C1048, Kind FT (fully tempered), Condition A (uncoated surfaces), Type 1 (transparent), Class 1 (clear) requirements.

- Provide products that have been tested for surface and edge compression according to ASTM C 1048 and for impact strength according to CPSC 16 CFR, part 1201 for Category II materials.

b.	Door cutouts: No drillings necessary

C.	Thickness:

1)	3/8 inch (10 mm).

d.	Exposed Edges: Flat polished.

- All wood, metal and framed glass sliding doors (SLID)

1.	System for wooden doors sliding along a wall or into pocket with track surface mounted, ceiling mounted or recessed. The materials include track and complete set(s) of accessories into a ingle kit.

2.	Track: Clear anodized aluminium finish with track's length of 98, 118", 157". Custom finish on request for project over 100 doors (custom fabrication)

- SLID S for doors up to 286 lbs (130kgs) with surface mounted brackets. Track' size of 1 3/4" (45mm) high x 1 3/8" (36mm) wide.

- SLID Retrac for doors up to 286 lbs (130kgs) with recessed brackets for recessed application. Track' size of 1 ¾” (45mm) high x 1 3/8" (36mm) wide.

- SLID POCKET for doors up to 200 lbs (90kgs) with recessed brackets for pocket door application. Track' size of 1 ¾” (45mm) high x 1 3/8" (36mm) wide.

- SLID TOP for doors up to 2861 lbs (130kgs) with recessed brackets for dropped ceiling application. Track’ size 1 ¾” (45mm) high x 2" (52mm) wide.

3.	Carriers: Top hung rollers (with Full Ball Bearings wheels), two per panel.

4.	Hardware including in the kit:

- 2 rollers / sliding door

- Brackets for surface mounted or recessed application

- Stoppers – Brakes

- 1 guide / sliding door (1" wide) running in groove in bottom of the door

- Upper Track

- End caps and wall brackets available on demand

5.	Door Panels: for doors up to the maximum weight capacity recommended by the manufacturer to reach an opening and closing force of maximum 5 lbs (23n) to fit ADA requirements.

a.	Thickness:

1)	From 1 3/8" thick wood

2.4    FABRICATION

- Fabricate all-glass or wood entrance components in sizes, profiles, and configurations indicated on the approved shop drawings.

- Fabricate doors and sidelights with required top and bottom fittings. Reinforce with steel sections or tie rods where required.

- Fabricate doors and sidelights to allow for minimum clearances and shim spacing around perimeter of assembly.

- Rigidly fit and secure joints and comers with internal reinforcement. Make joints and connections flush, hairline, and weatherproof.

PART 3 EXECUTION

3.1    EXAMINATION

- Do not begin installation until support and floor substrates have been properly prepared.

- Verify wall openings are ready to receive work of this section.

- Verify concealed overhead structural supports, are sized and located properly.

- Supporting structure must be level

- Insure finished floor under operable glass partition is leveled

- Verify opening dimensions prior to fabrication and assembly

- Notify architect of unsatisfactory conditions

3.2    PREPARATION

- Clean surfaces thoroughly prior to installation.

- Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

- Preparation of the opening shall conform to the criteria set forth per ASTM E 557 "Standard Practice for Architectural Application and Installation of Operable Partitions."

3.3    INSTALLATION

- Install in accordance with manufacturer's instructions.

- Comply with manufacturer's written installation instructions, Drawings, and approved Shop Drawings.

- Install glass partitions and accessories after other finishing operations, including painting, have been completed.

- Match glass partitions by installing panels from marked packages in numbered sequence indicated on instruction sheet.